## Slide 1
Electric field emission and local surface heating in plasma packed bed reactors having metal catalyst-impregnated dielectric beads*
Juliusz Kruszelnicki, Kenneth W. Engeling, John E. Foster, and Mark J. Kushner
University of Michigan, Ann Arbor, MI, 48109, USA
jkrusze@umich.edu, kenengel@umich.edu, jefoster@umich.edu, mjkush@umich.edu
71st Gaseous Electronics Conference
Portland, Oregon USA
November 2018
* Work supported by the DOE Office of Fusion Energy Science and the National Science Foundation.

## Slide 2: AGENDA
Plasma catalytic systems
Descriptions of the model and experiment
Polarization of catalysts
Electric field emission
Surface fluxes and heating
Concluding Remarks
GEC_2018
University of Michigan
Institute for Plasma Science & Engr.
Notes: Application for atm discharges

## Slide 3: PLASMA-CATALYTIC SYSTEMS
Plasmas in Packed Bed Reactors (PBRs) are used for gas reprocessing.
Dielectric provides electric field enhancement.
The catalysts in PBRs are metal particles (10-100 nm) impregnated onto dielectric beads.
Catalysts enable favorable reaction pathways by decreasing activation energy.
Plasma/catalytic synergy has been observed, but not yet explained.
University of Michigan
Institute for Plasma Science & Engr.
Kim et al. J. Phys. D. 42, 135210 (2009).
Kim et al. Eur Phys J Appl Phys 55, 13806 (2011)
GEC_2018
Notes: contribution

## Slide 4: RESEARCH ISSUES
Plasma discharge dynamics: How does presence of metallic particles affect DBD discharges in PBRs?
Formation of surface discharges: What processes produce additional plasma structures in catalyst-impregnated systems?
Surface fluxes: What species are delivered to the catalyst surface?
Surface heating: How is energy transferred to the catalyst and what are the sources?
University of Michigan
Institute for Plasma Science & Engr.
GEC_2018
X. Tu et al., Trans. Plasma Sci. 39, 2172, (2011).
Notes: Application for atm discharges

## Slide 5
MODEL: nonPDPSIM
2-D plasma hydrodynamic simulator over an unstructured mesh.
Poisson’s and continuity equations solved implicitly:
Local electron temperatures solved using the Boltzmann Equation:
Includes bulk fluid flow, gas heating, surface interactions, radiation transport and kinetics.
Poisson’s Equation
(gas, liquid and solids)
Surface Chemistry
and Charging
Radiation Transport
Electron Energy
Transport
Neutral Transport
Navier-Stokes
Neutral and Plasma
Chemistry
University of Michigan
Institute for Plasma Science & Engr.
GEC_2018
Notes: 5
5

## Slide 6: HEATING OF SOLIDS
Heating of solids is included by extending heat conduction term of temperature equation of plasma into solid materials.
Sources of heating of solids are fluxes of plasma produced species onto surface. Contributions by fluxes are:
Ion potential and kinetic energies (2).
Electron kinetic energy (3).
Electron emission (3).
GEC_2018
University of Michigan
Institute for Plasma Science & Engr.
Neutrals surface reactions (4).
UV (5).
Notes: Dielectric relaxation time of catalysts ~ 9e-15 s.

## Slide 7: MODEL GEOMETRIES
Reaction mechanism: N2/O2/H2O (78/21/1), 70 species, 1800 reactions.
Photoionization of O2 by radiation from N2**.
Mesh:
Full-scale: 13,000 nodes.
Close-up: 8,500 nodes.
Dielectric beads: εr = 8.
Catalysts: silver
Modeled as a dielectric with high conductivity.
εr = 10
σ = 100 Ω-1-cm-1
W = 5 eV
qthermal = 4.06 W-cm-1-K-1
Cp= 0.023 J-cm-3-K-1
Reflectance: 0.4
GEC_2018
University of Michigan
Institute for Plasma Science & Engr.
Notes: Humidity:

## Slide 8: DESCRIPTION OF EXPERIMENT
University of Michigan
Institute for Plasma Science & Engr.
Work by K. W. Engeling.
2-D Packed Bed Reactor:
Width: 0.8 cm
Length: 1 cm
Pin-to-planar electrodes.
7 dielectric rods.
Unipolar ns pulses.
GEC_2018
Silver (Ag) paint used to emulate metal catalysts.
Fast ICCD camera (5 ns exposure).
Notes: Application for atm discharges

## Slide 9: BASE CASE – DISCHARGE EVOLUTION
Plasma initiated at cathode tip.
Initial negative streamer enters lattice.
Dielectric barrier discharge:
Microdischarges form in gaps between beads due to field enhancement.
Surface ionization waves form.
Humid air, 1 atm
GEC_2018
Animation Slide
University of Michigan
Institute for Plasma Science & Engr.
Model and experiment (without catalyst)
Notes: Humidity:

## Slide 10: BASE CASE – DISCHARGE EVOLUTION
Gas/metal/dielectric triple points of catalysts produce electric field enhancement.
As microdischarge crosses gap, electrons seed triple point, producing a micro-streamer at the edges of catalyst.
Left: fast camera ICCD imaging of plasma near painted-on silver layers.
Humid air, 1 atm
GEC_2018
Animation Slide
University of Michigan
Institute for Plasma Science & Engr.
Notes: Humidity:

## Slide 11: POLARIZATION OF CATALYST PARTICLES
University of Michigan
Institute for Plasma Science & Engr.
Charges flow through metallic catalysts, accumulate at surfaces and produce additional field enhancement.
Electric fields ‘direct’ streamers towards the triple points.
Electric field between the head of the streamer (+, red at left) and catalyst (-, blue at left) continues increasing (peak ≈ 250 kV/cm).
GEC_2018
Animation Slide
t = 17-19 ns

## Slide 12: FIELD EMISSION: SHAPE OF CATALYSTS
University of Michigan
Institute for Plasma Science & Engr.
Sharper protrusions lead to higher local field enhancement.
With protruding catalyst, peak electric field increases from 240 to 400 kV-cm-1.
Higher E-field leads to field emission, seeding electrons for more localized microdischarges.
d
h
r
Anode
Cathode
GEC_2018
Animation Slide
t = 1.6 ns
Notes: Beta is the analogous to surface roughness.

## Slide 13: ELECTRIC FIELD EMISSION OF ELECTRONS
University of Michigan
Institute for Plasma Science & Engr.
Electric field enhancement (1< β <1000s) due to unresolved surface roughness (Fowler-Nordheim).
Electric Fields (up to 1000s of kV/cm) overcome catalyst work function (≈ 5 eV), leading to field emission.
Discharge formation dominated by field emission at high β.
GEC_2018
Animation Slide
t = 2.0 ns
t = 1.2 ns
Notes: Beta is the analogous to surface roughness.

## Slide 14: FORMATION OF SURFACE DISCHARGES
University of Michigan
Institute for Plasma Science & Engr.
E-field emission of electrons into gap can seed micro-plasma filaments when plasma would otherwise not form.
Similar to experimental trends – plasma does not form on surface of pure HY zeolite, but does when HY is impregnated with Ag particles.
 Kim et al. Plasma Chem Plasma Process 36, 45 (2016)
β=150
Zeolite, no catalyst
Zeolite, Ag catalyst
GEC_2018
Animation Slide
t = 6.0 ns

## Slide 15: FIELD ENHANCEMENT: FLUENCE
University of Michigan
Institute for Plasma Science & Engr.
Fluence: Time integrated flux.
Values in prentices: fluences (cm-2) at β = 10.
Reactive species with highest fluences: UV, e-, O2+, N2+, N2(v), N, O, OH, H.
Higher β leads to higher plasma conductivity, lower electron temperature near catalyst.
Lower dissociation rates produce lower fluence.
Pathway to selectivity: N2 dissociation, ionization requires higher energy than O2 – lower relative fluences of RNS than ROS.
GEC_2018
Notes: Beta is the analogous to surface roughness.

## Slide 16: POWER DEPOSITION
University of Michigan
Institute for Plasma Science & Engr.
Fractional and total power deposition to catalysts due to a single pulse.
Three distinct stages:
Electrons impact catalyst prior to streamer formation.
As streamer reaches catalyst, high potential drop leads to flux of energetic ions.
Neutral reactions dominate as conductive plasma forms near catalysts and in the afterglow.
GEC_2018
Contributions: Ions > Neutrals > Electrons > UV.
e-
Ion
Neutral

## Slide 17: CATALYST HEATING
University of Michigan
Institute for Plasma Science & Engr.
Total energy to catalyst per pulse of 3 μJ produced ∆T ≈ 0.002 K – requires 5×104 pulses for increase of 100 K.
Heating terms increased by x 1,000 to speed computation. Gas temperature reset after each pulse.
Average catalyst temperature equilibrates at ≈ 525 K, typical light-off condition for ammonia production.
Animation Slide
GEC_2018
frequency = 10 kHz
t = 0.15 s

## Slide 18: CONCLUDING REMARKS
Charge redistribution within the metal leads to catalysts providing additional field enhancement, guiding discharges toward catalyst.
Field strengths are high enough to induce electric field emission which may explain surface plasmas observed in experiments.
Catalysts protruding from surfaces further increase field enhancement, field emission.
Emitted electrons increase plasma conductivity near catalyst, decrease electron temperature and fluences.
Ions are the main contributors to surface heating of catalysts.
Plasma can bring catalyst temperature above light-off condition for chemical conversion.
GEC_2018
University of Michigan
Institute for Plasma Science & Engr.